## Slide 1: Software tools for high-throughput CALPHAD from first-principles data
Axel van de Walle
Ruoshi Sun
Qijun Hong
Sara Kadkhodaei
Funding support:
N00014-16-1-3124
N00014-17-1-2202
DMR-1505657
Acknowledgements:
  Thanks to Vidvuds Ozolins and Ursula Kattner for helpful comments.

## Slide 2: What does a typical phase diagram look like?
© ASM international
© ASM international
Z.K. Liu
et al. (2000)
Cao et al. (2007)
All phases are superstructures of a common lattice?
If you are lucky!
Complex mix of very different crystal structures:
More typical!
bcc
hcp
s
c

## Slide 3: Spectrum of ab initio thermodynamics methods
T = 0K Energies
Dilute defect calculations
Cluster expansion
Cluster expansion
with lattice dynamics
Computational cost
Information or Accuracy
?
SQS + CALPHAD
Mid-range methods useful for:
Exploratory screening (high-throughput + solid solutions)
Starting point in CALPHAD modeling

## Slide 4: SQS + CALPHAD Method
Free energy =
End member free energy
+ formation enthalpy: polynomial in composition
+ ideal solution formation entropy
+ short-range-order correction.
Experimental SGTE data
Special Quasirandom Structure
(SQS) formation energies.
Except for SRO correction, not a new method – Works by various research groups:
Zunger, Morgan, Liu, Arroyave, Asta, Wolverton, Sluiter, Crivello, Joubert,
among many others.
But we will “push it” further!

## Slide 5: SQS + CALPHAD method
Well-known and apparently straightforward method, however:
  Becomes less trivial when considering general multicomponent ordered phases with multiple sublattices. Why?
    SQS generation is more difficult!
    End members are not in SGTE database: Need to calculate formation free energies.
  Have to properly handle the issue of mechanical stability!
    Most phases (even bcc,fcc,hcp) become mechanically unstable in at least some composition range.
    The end members reference energies are often mechanically unstable.

## Slide 6
SQS Database
Interaction
Enumeration
Site Occupation
Enumeration
Statistical Fit
SGTE
Element
Database
Solution
Formation
Energy
Thermodynamic
Model
“.TDB” file
“mcsqs” code
Pandat, ThermoCalc, OpenCalphad,…
“sqs2tdb” code
Cross-section re-assembly
3D phase diagram
Software framework
Paraview, …
TST Tools
VASP
“robustrelax” code
Candidate lattices + composition

## Slide 7: SQS for multi-component multi-sublattice systems
Need to generate SQSs that span the composition range of each sublattice with various levels (0,1,2,3,… ) of accuracy. Examples:
AC
BC
AD
BD
0
0
x
y
1
2
2
0
0
1
2
2
1
1
3
4
4
2
2
4
4
4
2
2
4
4
4
Rocksalt A1-xBxC1-yDy
0
1
2
3
4
0
0
1
1
2
2
2
2
2
A
B
C
bcc, fcc, hcp
4
4

## Slide 8: Reference free energies
Composition
Free energy
Typically: Compute vibrational free energy contributions for end members only.
Intermetallic phase

## Slide 9: SQS Database
fcc | A1 |  | Cuprite | C3
bcc | A2 |  | Rutile | C4
hcp | A3 |  | MgCu2 | C15
b-Sn | A5 |  | w | C32
c | A12 |  | Heusler | D022
Cr3Si | A15 |  | Fe3Al | D03
Rocksalt | B1 |  | s | D8b
CsCl | B2 |  | Perovskite | E21
Zincblende | B3 |  | AuCu | L10
CuPt | B22 |  | g | L12
Zintl | B32 |  | Heusler | L21
Fluorite | C1 |  | Zirconia (tet.) | 
Pyrite | C2 |  | … | 
c phase with sublattice disorder
5-component fcc solid solution,
Rocksalt structure with disorder on both sublattices
s phase with disorder on all 3 of its sublattices.
Current list
Examples
(still growing…)
Each entry represent 5 to 10 SQS!

## Slide 10: Liquid and gas phases?
Can use SGTE data for end members.
We add ab initio liquid solution formation enthalpy from a short MD run above highest melting point of end members.
  This is needed to avoid systematic bias in solid-liquid free energy differences.
  Inaccurate is liquid short-range orders…
  For a better method, see Q.-J. Hong and A. van de Walle. “Solid-liquid coexistence in small systems: A statistical method to calculate melting temperatures.” J. Chem. Phys., 139:094114, 2013.
Gas phase: Use experimental or ideal gas.

## Slide 11: Mechanically unstable phases: Why bother?
If one only looks at stable regions and relies on extrapolation:
  The extrapolated free energies may accidentally lie below the free energy of stable phases
  Extrapolation from different directions in composition space may disagree.
To keep the spirit of the CALPHAD method.
Extremely useful in the context of cluster expansions as well.

## Slide 12: Handling mechanical instabilities: Curvature-based partitioning of phase space
Positive-definite Hessian
Hessian with at least one negative eigenvalue
(fcc)
(bcc)
Example of W
van de Walle, Hong, Kadkhodaei and Sun., “The free energy of mechanically unstable phases.”, Nature Commun., 6:7559, 2015.
Notes: Basic idea: think of the an alloy’s energy surface: potential energy as a function of atomic position and cell parameters (what I call the vector x in this picture). In a mechanically stable region, where that surface has a positive curvature (in red), everybody agrees on what to do: you start at some “unrelaxed” structure x^u and you fully relax to find the nearest local minimum x^r. Then you can use a standard harmonic model to represent the free energy associate with that red “pocket” of stability.
When you have a mechanically unstable region (with at least one negative curvature), it is then natural to assign the complement of those stable red regions to the mechanically unstable phase in blue. If you then follow the same logic, starting from an unrelaxed structure x^u, you would want to find the minimum x^r in the blue region. Due to the instability, the minimum is always at the boundary. At the boundary, by definition, the minimum curvature is exactly zero [because it’s the transition between positive and negative curvature]. So the minimum, constrained to the blue region, is at an inflection point.

## Slide 13: Advantages of this definition
Consistent with the usual notion of a stable basin.
Can use a simple harmonic expansion about a point at the boundary (xsr).
  By definition, only a finite number of modes are unstable at that point and a finite number of modes has a negligible contribution to the free energy.
  Points inside hs do not have this property: they are associated with an infinite number of unstable modes.
The inflection point is a natural extension of a local minimum: “inflection-detection” method.
k
n
k
n
Phonon dispersion curve
at boundary of hs
Phonon dispersion curve
inside hs
Notes: This definition of the energy of a mechanically unstable phase is completely consistent

## Slide 14: Onset of mechanical instability
The inflection point is a natural extension of a local minimum.
dV/dx
x
Why? When a local minimum disappears, it does so by joining an inflection point (and a local maximum):
Changes in potential V as a function of
position x and
some external variable a = composition, T, P, …

## Slide 15: Extrapolation behavior and compatibility with SGTE data

## Slide 16: Extrapolation: A closer look

## Slide 17: The case of fcc W - bcc W
(Adapted from Ozolins (2009))

## Slide 18: Compatibility with SGTE
* : fully relaxed
+ : inflection-detection
 : symmetry-constrained

## Slide 19: Compatibility with SGTE
* : fully relaxed
+ : inflection-detection
 : symmetry-constrained

## Slide 20: Compatibility with SGTE
* : fully relaxed
+ : inflection-detection
 : symmetry-constrained

## Slide 21: How to find the minimum energy in mechanically unstable region of phase space?
Look for boundary solution:
Minimum energy subject to zero minimum curvature.
Equivalent formulation:
Minimize energy,
moving perpendicularly to gradient of min curvature.
Can be implemented via a dimer-like method, see:
van de Walle, Kadkhodaei Sun & Hong, “Epicycle method for elasticity limit calculations”, Phys. Rev. B 95 144113 (2017).

## Slide 22: How to find minimum xsr in region hs?
Minimum curvature
determination:
Ionic positions
optimization:

## Slide 23: General solution to mechanical instabilities?
Covers phases that are mechanically unstable and truly unstable “in the real world”.
  It is a formal definition (well-defined free energies) based on logical considerations but it is still a choice.
  Nice extrapolation behavior.
  It happens to agree well with historically accepted values.
Not aimed, on its own, at handling mechanically unstable phonon modes that are dynamically stabilized by anharmonicity.
  Sampling of many configurations still needed.
  See Kadkhodaei, Hong & van de Walle, “Free energy calculation of mechanically unstable but dynamically stabilized bcc titanium”, Phys. Rev. B 95, 064101 (2017) for a solution.

## Slide 24: Short-range order effects…
Short-range order is (usually) a smaller contributions to free energy differences than differences in coordination number.
Equilibria between two different crystal structures usually involves phases that are far from ordering transition on their respective sublattices.
Common tangent masks short-range ordered regions.
Free energy
Composition

## Slide 25: Short-range order correction
Starting point: Cluster Variation Method (CVM) within the pair approximation.
Truncated expansion: Polynomial in composition
Temperature-dependence: Solve CVM equations exactly for middle composition, scale solution to match first-order behavior at all compositions.
Why use such a simple scheme?
Comes “for free” (no additional ab initio calc needed)
We use it mostly in the near-random solution limit, so the expansion is accurate
Fits well within the “TDB” file format.

## Slide 26: How well does this SRO model work?
With SRO correction
Without SRO correction
Experiment (Fact Sage/SGnoble)
Calculations:

## Slide 27: Some examples…

## Slide 28: Re-Ru-W
E.M Savitskii (1975)
This work.
hcp
bcc
s
hcp
bcc
s
c
© ASM international

## Slide 29: Ir-Re-W: Binaries subsystems Full ternary system

## Slide 30: Binary subsystems: Re-W
Z.K. Liu et al. (2000)
© ASM international
This work.
hcp
bcc
c
s
hcp
bcc
c
s
L
L

## Slide 31: Binary subsytems: Ir-W
H. Okamoto et al. (1990)
© ASM international
This work.
fcc
bcc
s
hcp
L
fcc
bcc
s
hcp
L

## Slide 32: Binary subsytems: Ir-Re
H. Okamoto et al. (1990)
© ASM international
This work.
fcc
hcp
L
fcc
hcp
L

## Slide 33: Ir-Re (continued) with vibrational formation free energy
fcc
hcp
L
fcc
hcp
L
H. Okamoto et al. (1990)
This work.

## Slide 34: Isothermal section: Ir-Re-W
E.M Savitskii (1975)
© ASM international
This work.
hcp
bcc
fcc
c
s
hcp
bcc
fcc
c
s
hcp

## Slide 35: The Ir-Re-W phase diagram

## Slide 36: Cu-Pt-W

## Slide 37: Ru-Ta-W
hcp
bcc
B2
Ga3Pt5
T = 2000oC

## Slide 38: Conclusion
We have presented
A simple method with surprisingly good predictive power.
A novel, theoretically justified and convenient definition of the free energy of mechanically unstable phases.
New software tools (included in ATAT) that allow you to take advantage of the above.
See the new ATAT forum: http://alum.mit.edu/www/avdw/forum/
>600 users, hundreds of posts…